## Slide 1
Electron-phonon Coupling and Charge Excitations
in Cuprate Superconductors
Qisi Wang (I21 user)
August 4th 2022
Magnetic Materials Group
Diamond, SEMINAR

## Slide 2
2020: room temperature superconductivity in C-S-H
E. Snider et al., Nature 586, 373 (2020)
Recent breakthrough

## Slide 3
2019: superconductivity in
infinite-layer nickelates
2020: room temperature superconductivity in C-S-H
E. Snider et al., Nature 586, 373 (2020)
D. Li et al., Nature 572, 624 (2019)
Recent breakthrough

## Slide 4
LaSrNiO2
Nickelates
Pickard et al., Annu. Rev. Condens. Matter Phys. 11, 57 (2020)
Cuprates – highest Tc at ambient pressure

## Slide 5
Ubiquitous charge order in hole-doped cuprates
Charge order in all hole-doped cuprates
R. Comin & A. Damascelli, Annu. Rev. Condens. Matter Phys 7, 369 (2016)
General phase diagram

## Slide 6
t
U
J ~ -2t2/U
Spin-charge stripe phase in doped Mott insulators
J. M. Tranquada et al., Nature 375, 561 (1995)
Real space

## Slide 7
charge
modulation
spin
modulation
δcharge= 2 δspin ~ ¼
J. M. Tranquada et al., Nature 375, 561 (1995)
Reciprocal space
Diffraction evidence of charge-spin stripe
Real space

## Slide 8
Symmetry of charge order: stripe or checkerboard?
R. Comin et al., Science 347, 1335 (2015)
Reciprocal space
Real space

## Slide 9
Lifting the charge-stripe domain degeneracy
J. Choi, Q. Wang et al., Phy. Rev. Lett. 128, 207002 (2022)
LSCO

## Slide 10
Lifting the charge-stripe domain degeneracy
H
K
J. Choi, Q. Wang et al., Phy. Rev. Lett. 128, 207002 (2022)

## Slide 11
Lifting the charge-stripe domain degeneracy
H
K
H
K
J. Choi, Q. Wang et al., Phy. Rev. Lett. 128, 207002 (2022)

## Slide 12
Lifting the spin-stripe domain degeneracy
G. Simutis, J. Küspert, Q. Wang et al., arXiv: 2204.02304

## Slide 13
2D SC state & 3D uniform SC
Q. Li et al., PRL 99, 067001 (2007)
Pair-density-wave (PDW) & charge-density-wave (CDW)
Why is interlayer Josephson coupling frustrated?

## Slide 14
Real-space schematic of PDW and CDW stripes
J. Choi, Q. Wang et al., PRL 128, 207002 (2022)
2D SC state & 3D uniform SC
Pair-density-wave (PDW) & charge-density-wave (CDW)
Q. Li et al., PRL 99, 067001 (2007)

## Slide 15
S. A. Kivelson et al., Nature 393, 550 (1998)
Transverse stripe fluctuation magnitude
2D electron motion due to stripe fluctuations
J. Zaane et al., Science 286, 251(1999)
Transverse stripe fluctuation

## Slide 16
M. Rossi et al., Nat. Phys. (2022)
S. Lee et al., PRL 122, 147601 (2019)
Ba(Ni,Co)2As2
Charge order in nickelates and pnictides systems
C. Tam, J. Choi, X. Ding, et al., ArXiv: 2112.04440
Ni112 superconductor
G. Krieger et al., PRL129, 027002 (2022)

## Slide 17
Microscopic mechanism
Is charge order a spontaneous symmetry breaking?
What is the role of the electron-phonon/lattice interaction?
Outstanding questions about cuprate charge order
Which phonon mode couples most strongly to charge order

## Slide 18
Q. Wang et al., PRL 124,187002 (2020)
O
La2CuO4
La-214 cuprates
Cu
O
HTT, C4 symmetry
La
Ba/Sr

## Slide 19
Q. Wang et al., PRL 124,187002 (2020)
Cu
O
HTT, C4 symmetry
La2-x (Sr,Ba)x CuO4
La2CuO4
hole p
(LSCO)
(LBCO)
Access to entire phase diagram
La
Ba/Sr

## Slide 20
Q. Wang et al., PRL 124,187002 (2020)
La
Ba/Sr
Cu
O
HTT, C4 symmetry
La2-x (Sr,Ba)x CuO4
La2CuO4
hole p
(LSCO)
(LBCO)
Charge order in La-214 cuprates

## Slide 21
J. M. Tranquada, AIP Conf. Proc. 1550, 114 (2013)
The 1/8 Tc anomaly
LSCO
LBCO
Compound dependent 1/8 Tc anomaly

## Slide 22
Q. Wang et al., PRL 124,187002 (2020)
THT
HTT
T
J. M. Tranquada, AIP Conf. Proc. 1550, 114 (2013)
LSCO & LBCO: different crystal structure
La
Ba/Sr
Cu
O
HTT, C4 symmetry

## Slide 23
Q. Wang et al., PRL 124,187002 (2020)
C4 symmetry broken
THT
HTT
T
LTO
LSCO
J. M. Tranquada, AIP Conf. Proc. 1550, 114 (2013)
LSCO & LBCO: different crystal structure
La
Ba/Sr
Cu
O
HTT, C4 symmetry

## Slide 24
Q. Wang et al., PRL 124,187002 (2020)
C4 symmetry broken
THT
LTT
HTT
T
TLT
LTO
LSCO
LBCO
J. M. Tranquada, AIP Conf. Proc. 1550, 114 (2013)
LSCO & LBCO: different crystal structure
La
Ba/Sr
Cu
O
HTT, C4 symmetry

## Slide 25
Q. Wang et al., PRL 124,187002 (2020)
C4 symmetry broken
THT
LTT
HTT
T
TLT
LTO
LSCO
LBCO
Top view
LTO
LTT
Stripes
J. M. Tranquada, AIP Conf. Proc. 1550, 114 (2013)
LSCO & LBCO: different crystal structure
La
Ba/Sr
Cu
O
HTT, C4 symmetry

## Slide 26
Q. Wang et al., PRL 124,187002 (2020)
C4 symmetry broken
THT
LTT
HTT
T
TLT
LTO
LSCO
LBCO
Top view
LTO
LTT
Stripes
J. M. Tranquada, AIP Conf. Proc. 1550, 114 (2013)
LSCO & LBCO: different crystal structure
La
Ba/Sr
Cu
O
HTT, C4 symmetry

## Slide 27
La2CuO4
Isovalent
hole
(Eu-LSCO)
(Nd-LSCO)
La2-x-y (Nd,Eu)y (Sr)x CuO4
Q. Wang et al., PRL 124,187002 (2020)
LSCO & LBCO: different crystal structure
La
Eu/Nd
Ba/Sr
Cu
O
HTT, C4 symmetry

## Slide 28
LTT grows faster than charge order
Charge order is driven by the LTT phase?
A. Achkar et al., Science 351, 576 (2016)
Resonant elastic x-ray scattering (REXS) results
Tco <= TLTT
Eu-LSCO
Nd-LSCO
LBCO
LTT & charge order

## Slide 29
XAS (absorption) & RIXS process
Sensitive to electronic correlations: charge, spin…
Resolve energy and momentum
Polarization selections: spin flip/non-flip
Resonant inelastic x-ray scattering (RIXS)
Excitation probed by RIXS
Excitations in infinite-layer nickelates
at Ni L-resonance
L. J. P. Ament et al., Rev. Mod. Phys. 83, 705 (2011)
H. Lu et al., Science 383, 213 (2021)

## Slide 30
RIXS for diffraction
Excitations in infinite-layer nickelates
at Ni L-resonance
H. Lu et al., Science 383, 213 (2021)
Raw RIXS spectrum
elastic
magnon
dd
Compared to REXS: inelastic process are filtered
-- lower background
Q. Wang et al., PRL 124,187002 (2020)

## Slide 31
ADRESS, Swiss Light Source, Switzerland
I21, Diamond Light Source, UK
ID32, Eur. Synchrotron Rad. Facility, France
RIXS beamlines

## Slide 32
H-scan of elastic scattering
Q. Wang et al., PRL 124,187002 (2020)
h
k
Temperature evolution of charge order in Eu-LSCO
TLTT = 125 K

## Slide 33
Peak intensity I vs T
Charge correlations outside LTT:
Spontaneous symmetry breaking
REXS-defined onset: probing limit
RIXS-probing limit between 200~300 K
No clear onset
Q. Wang et al., PRL 124,187002 (2020)
No clear onset for charge order detected

## Slide 34
Peak intensity vs correlation length
Scaling behavior:
constant scattering volume
Q. Wang et al., PRL 124,187002 (2020)
intensity and correlation length scaling

## Slide 35
Peak intensity vs correlation length
Scaling behavior:
constant scattering volume
intensity and correlation length scaling
Q. Wang et al., PRL 124,187002 (2020)

## Slide 36
Lee et al., 119, PNAS e2119429119 (2022)
New REXS results with more carefully background analysis
Generic scaling behavior of charge order

## Slide 37
Microscopic mechanism
Is charge order a spontaneous symmetry breaking?
What is the role of the electron-phonon/lattice interaction?
Outstanding questions about cuprate charge order
Which phonon mode couples most strongly to charge order

## Slide 38
t
U
J ~ -2t2/U
Spin-charge stripe phase in doped Mott insulators
J. M. Tranquada et al., Nature 375, 561 (1995)
Real space

## Slide 39
X. Zhu et al., PNAS 112, 2367 (2015)
Weber et al., PRL 2011
CDW due to Q-dependent EPC
(Electron-phonon coupling)
NbSe2
Charge order due to electron-phonon coupling

## Slide 40
Inter-band e-ph
scattering
ARPES kink
EPC constant
Hofmann et al., New J. Phys. 11, 125005 (2009)
Lanzara et al., Nature, 412, 510 (2001)
ARPES as a probe of e-ph coupling

## Slide 41
Inter-band e-ph
scattering
ARPES kink
EPC constant
Hofmann et al., New J. Phys. 11, 125005 (2009)
Lanzara et al., Nature, 412, 510 (2001)
Which bosonic mode? Phonon? Magnon?
q-dependence of M(k,q)?
Which phonon?
ARPES as a probe of e-ph coupling

## Slide 42
LBCO-1/8
D. Reznik et al., Nature 440, 1170 (2006)
Underdoped YBa2Cu3O6.6
M. Le Tacon et al., Nature Physics 10, 52 (2013).
Soft phonon in cuprates

## Slide 43
LBCO-1/8
D. Reznik et al., Nature 440, 1170 (2006)
Underdoped YBa2Cu3O6.6
M. Le Tacon et al., Nature Physics 10, 52 (2013).
Phonon self-energy
Soft phonon in cuprates

## Slide 44
L. Braicovich et al., PRR 2, 023231 (2020)
RIXS process to generate phonons

## Slide 45
i) Electron-phonon coupling
ii) Core-hole life-time
RIXS phonon intensity
L. Braicovich et al., PRR 2, 023231 (2020)
RIXS process to generate phonons

## Slide 46
Anomalous cuprate phonons probed by RIXS
Bi2212
W. S. Lee, K.-J. Zhou et al., Nat. Phys. 17, 53 (2021)
Bi2201
J. Li et al., PNAS 117, 16219 (2020)
LSCO
J. Q. Lin et al., PRL124, 207005 (2020)
Cuprate phonon studies enabled by the ultrahigh resolution at I21

## Slide 47
I21: ultrahigh resolution RIXS beamline
I21, Diamond Light Source, UK

## Slide 48
Q. Wang et al., Sci. Adv. 7, eabg7394 (2021)
Low-energy excitation mode at ~ 60 meV
Cu L-edge

## Slide 49
Cu
O
BS phonon eigenvector
at Q = (0.25,0)
Q. Wang et al., Sci. Adv. 7, eabg7394 (2021)
Assignment: bond stretching (BS) phonon mode
Cu L-edge

## Slide 50
Q. Wang et al., Sci. Adv. 7, eabg7394 (2021)
Phonon lifetime shortening near QCDW

## Slide 51
BS phonon anomaly
Q. Wang et al., Sci. Adv. 7, eabg7394 (2021)
Softening around QCDW
At high T due to charge correlations
BS phonon softening

## Slide 52
BS phonon anomaly
Enhanced e-phonon coupling at low T
Q. Wang et al., Sci. Adv. 7, eabg7394 (2021)
Softening around QCDW
At high T due to charge correlations
Anomalous BS phonon intensity

## Slide 53
Softening around QCDW
At high T due to charge correlations
BS phonon anomaly
Enhanced e-phonon coupling at low T
Occurs within the LTT phase
Q. Wang et al., Sci. Adv. 7, eabg7394 (2021)
Anomalous BS phonon intensity

## Slide 54
Q. Wang et al., Sci. Adv. 7, eabg7394 (2021)
Anomalous BS phonon intensity

## Slide 55
Microscopic mechanism
Is charge order a spontaneous symmetry breaking?
What is the role of the electron-phonon/lattice interaction?
Outstanding questions about cuprate charge order
Q. Wang et al., Science Advances 7, eabg7394 (2021).
EPC contributes significantly in addition to the electronic correlations
to the long-range charge order formation.

## Slide 56
Microscopic mechanism
Is charge order a spontaneous symmetry breaking?
What is the role of the electron-phonon/lattice interaction?
Outstanding questions about cuprate charge order
Which phonon mode couples most strongly to charge order

## Slide 57
EPC through lower-lying phonons?
Apical
Buckling
Bond-
stretching
Giustino et al., Nature 452, 975 (2008)
Low-energy phonons may also couple strongly to charge order
Why lower-energy phonons
Anazai Sci. Rep. (2017)

## Slide 58
EPC through lower-lying phonons?
Apical
Buckling
Bond-
stretching
Giustino et al., Nature 452, 975 (2008)
Low-energy phonons may also couple strongly to charge order
Low-energy phonons could possibly influence pairing
Why lower-energy phonons
Anazai Sci. Rep. (2017)
Johnston PRB 82, 064513 (2010)

## Slide 59
EPC through lower-lying phonons?
Apical
Buckling
Bond-
stretching
Giustino et al., Nature 452, 975 (2008)
Bands across the Fermi level have significant O 2px,y character
Low-energy phonons may also couple strongly to charge order
Low-energy phonons could possibly influence pairing
Why O K-edge RIXS
Why lower-energy phonons
Anazai Sci. Rep. (2017)
LSCO XAS
Chen PRL 66, 104 (1991)
Johnston PRB 82, 064513 (2010)

## Slide 60
EPC through lower-lying phonons?
Apical
Buckling
Bond-
stretching
Giustino et al., Nature 452, 975 (2008)
Bands across the Fermi level have significant O 2px,y character
Low-energy phonons may also couple strongly to charge order
Low-energy phonons could possibly influence pairing
Higher energy resolution
Why O K-edge RIXS
Why lower-energy phonons
Anazai Sci. Rep. (2017)
LSCO XAS
Chen PRL 66, 104 (1991)
Johnston PRB 82, 064513 (2010)

## Slide 61
EPC through lower-lying phonons?
Apical
Buckling
Bond-
stretching
Giustino et al., Nature 452, 975 (2008)
Bands across the Fermi level have significant O 2px,y character
Low-energy phonons may also couple strongly to charge order
Low-energy phonons could possibly influence pairing
Longer core-hole lifetime — larger RIXS phonon cross sections
Higher energy resolution
Why O K-edge RIXS
Why lower-energy phonons
Anazai Sci. Rep. (2017)
LSCO XAS
Chen PRL 66, 104 (1991)
Johnston PRB 82, 064513 (2010)

## Slide 62
EPC through lower-lying phonons?
Apical
Buckling
Bond-
stretching
Giustino et al., Nature 452, 975 (2008)
Bands across the Fermi level have significant O 2px,y character
Low-energy phonons may also couple strongly to charge order
Low-energy phonons could possibly influence pairing
Longer core-hole lifetime — larger RIXS phonon cross sections
Single magnon disallowed — phonons are more isolated
Higher energy resolution
Why O K-edge RIXS
Why lower-energy phonons
Anazai Sci. Rep. (2017)
LSCO XAS
Chen PRL 66, 104 (1991)
Johnston PRB 82, 064513 (2010)

## Slide 63
I21, Diamond Light Source, UK
I21: ultrahigh resolution RIXS beamline

## Slide 64
LV (E//ab)
LH (E//c)
ZRS
UHB
px,y
3d9L->1s3d9
pz
3d9->1s3d10
Grazing-in XAS
XAS: significant O pxy orbital character
Resonance at the Zhang-Rice singlet energy

## Slide 65
Fitting and assignment of RIXS excitations
0
0.5
1
1.5
2
2.5
3
-0.5
Energy loss (eV)
Intensity (a.u.)
dd-excitations
Bi-magnon
Elastic line
phonons

## Slide 66
Fitting and assignment of RIXS excitations
0
0.5
1
1.5
2
2.5
3
-0.5
Energy loss (eV)
Intensity (a.u.)
dd-excitations
Bi-magnon
Elastic line
phonons
h = 0.27
h = 0.18
O K-edge
Cu L-edge

## Slide 67
Fitting and assignment of RIXS excitations
0
0.5
1
1.5
2
2.5
3
-0.5
Energy loss (eV)
Intensity (a.u.)
dd-excitations
Bi-magnon
Elastic line
phonons
h = 0.27
h = 0.18
Excitation energy
Cu L-edge
O K-edge
Bond stretching (half breathing)
DFT
Optical
Chaplot et al., PRB 52, 7230 (1995)
Giustino et al., Nature 452, 975 (2008)

## Slide 68
Fitting and assignment of RIXS excitations
0
0.5
1
1.5
2
2.5
3
-0.5
Energy loss (eV)
Intensity (a.u.)
dd-excitations
Bi-magnon
Elastic line
phonons
h = 0.27
h = 0.18
Buckling A1g
Excitation energy
Cu L-edge
O K-edge
Bond stretching (half breathing)
DFT
Optical
Chaplot et al., PRB 52, 7230 (1995)
Giustino et al., Nature 452, 975 (2008)

## Slide 69
Fitting and assignment of RIXS excitations
0
0.5
1
1.5
2
2.5
3
-0.5
Energy loss (eV)
Intensity (a.u.)
dd-excitations
Bi-magnon
Elastic line
phonons
h = 0.27
h = 0.18
Buckling B1g
Buckling A1g
Excitation energy
Cu L-edge
O K-edge
Bond stretching (half breathing)
DFT
Optical
Chaplot et al., PRB 52, 7230 (1995)
Giustino et al., Nature 452, 975 (2008)

## Slide 70
Fitting and assignment of RIXS excitations
0
0.5
1
1.5
2
2.5
3
-0.5
Energy loss (eV)
Intensity (a.u.)
dd-excitations
Bi-magnon
Elastic line
phonons
h = 0.27
h = 0.18
Buckling B1g
Buckling A1g
Excitation energy
Cu L-edge
O K-edge
Bond stretching (half breathing)
Acoustic mode?
DFT
Optical
Chaplot et al., PRB 52, 7230 (1995)
Giustino et al., Nature 452, 975 (2008)

## Slide 71
T
TLTT = 125 K
Phonon dispersion and intensity in Eu-LSCO
Q. Wang, X. Hong et al., in preparation

## Slide 72
T
TLTT = 125 K
T
TLTT = 125 K
Stretching mode
~20 meV mode
Buckling
mode
Phonon dispersion and intensity in Eu-LSCO
Bond-stretching mode does not peak at QCDW
20 meV and buckling modes exhibit much sharper peak at QCDW, which do not correlate with LTT transition
No softening resolved for the 20 meV and buckling modes
Q. Wang, X. Hong et al., in preparation

## Slide 73
Phonon dispersion and intensity in Eu-LSCO
~20 meV mode
Stretching mode
Q. Wang, X. Hong et al., in preparation
Xunyang Hong, ETH & UZH

## Slide 74
Phonon dispersion and intensity in LSCO
Huang et al., PRX 11, 041038 (2021)
Optimally doped LSCO

## Slide 75
Difference between LSCO and Eu-LSCO
Huang et al., PRX 11, 041038 (2021)
Optimally doped LSCO
1/8 doped Eu-LSCO
Q. Wang, X. Hong et al., in preparation
W. S. Lee, K.-J. Zhou et al., Nat. Phys. 17, 53 (2021)
Eu-LSCO?
LSCO?

## Slide 76
Microscopic mechanism
Charge order heralds a spontaneous symmetry breaking
Electron-phonon interaction promote the charge order development
Summary
Q. Wang et al., Science Advances 7, eabg7394 (2021)
Q. Wang et al., Physical Review Letters 124, 187002 (2020)
EPC most strongly affects the bond-stretching phonon in Eu-LSCO
Sharp enhancement of the ~20 meV phonon mode can be captured by Fermi surface nesting
Q. Wang, X. Hong et al., in preparation

## Slide 77: Acknowledgement
Henrik M. Rønnow
Wenliang Zhang
Thorsten Schmitt
Deepak Mukkattukavil
Yasmine Sassa
Jaewon Choi
Abhishek Nag
Mirian Garcia-Fernandez
Stefano Agrestini
Ke-Jin Zhou
Tohru Kurosawa
Naoki Momono
Migaku Oda
Yoji Koike
S. M. Haidar
Yao Shen
Jun Zhao
Karin von Arx
Xungyang Hong
Masafumi Horio
Oleh Ivashko
Christian Matt
Johan Chang
Kurt Kummer
Nick B. Brooks
The European Sychrotron
Sunseng Pyon
Tomohiro Takayama
Hidenori Takagi
Tadashi Adachi
Sophia University
Niels Bech Chirstensen