## Slide 1: O K-edge phonon in Eu-LSCO-p125
Beamline: I21
Proposal: MM29011-1
Time: 2021.10.08-11 (9 shifts)

## Slide 2: Software info.
DawnDiamond-2.23.0.v20211005-0856-win32.x86_64-inst

## Slide 3
Dispersion and slope from #206272, phonon energy scan on C-tape
This is for the fast scans that did not take the C-tape. Save the processed elastic line data

## Slide 4
Dispersion = 0.0037176 eV/pxl, get elastic peak pos. at each energy, export the pos. from Dawn, then manually fit
Energy dispersion = 1/268.99302 = 0.0037176 eV/pxl
#206272

## Slide 5
Slope, take the average = -0.0381
#206272

## Slide 6
Ep = 527.46; % photon energy
tth = 154; % scattering angle
lat_a = 3.79; % lattice parameters
lat_b = lat_a;
lat_c = 13.1;
theta0 = -0.94; % theta offset
phi = -1.4;
phi0 = -1.4;
theta = 15:0.5:40; % theta for quick scan
[qh,qk,ql] = q_cal_RIXS(Ep,tth,lat_a,lat_b,lat_c,theta,theta0,phi,phi0);
theta = theta';
qh = qh';
qk = qk';
ql = ql';
qq = [theta,qh,qk,ql];
Calculate (h, k, l), (for fast scans)
Ep = 527.46; % photon energy
tth = 154; % scattering angle
lat_a = 3.79; % lattice parameters
lat_b = lat_a;
lat_c = 13.1;
theta0 = -0.94; % theta offset
phi = -6.4:0.5:3.6;
phi0 = -1.4;
theta = 27;
[qh,qk,ql] = q_cal_RIXS(Ep,tth,lat_a,lat_b,lat_c,theta,theta0,phi,phi0);
theta = theta';
phi = phi';
qh = qh';
qk = qk';
ql = ql';
qq = [phi,qh,qk];

## Slide 7
Fast h-scan (50 um slit) #[206342:206392]
Same setting for fast phi-scan (50 um slit) #[206393:206413,206416,206417]

## Slide 8
Fast h-scan (50 um slit) #[206342:206392]
Same setting for fast phi-scan (50 um slit) #[206393:206413,206416,206417]

## Slide 9
High-res Q-scan (20 um slit) 206426 until 206554

## Slide 10
High-res Q-scan (20 um slit) 206426 until 206554
Correlation energy range: -0.1,0.1

## Slide 11
Dispersion and slope from #206684, phonon energy scan on C-tape
This is for the ultra-high-res data

## Slide 12
Dispersion = 0.00236855 eV/pxl, get elastic peak pos. at each energy, export the pos. from Dawn, then manually fit
Energy dispersion = 1/422.19916 = 0.00236855 eV/pxl
#206684
This is for the ultra-high-res data

## Slide 13
Slope, take the average = -0.03212
#206684
This is for the ultra-high-res data

## Slide 14
Ultra-high-res Q-scan (20 um slit) 206692 until 206723
This is for the ultra-high-res data

## Slide 15
Ultra-high-res Q-scan (20 um slit) 206692 until 206723
This is for the ultra-high-res data
Correlation energy range: -0.1,0.1

## Slide 16
Determine resolution for high-res RIXS, #[206273:206277]
Average FWHM = 6.1247 pxl (from 5 C-tap scans)
Res = 6.12473 pxl* 0.0037176 eV/pxl = 22.77 meV
This is Gauss fitting, I will manually do Voigt fitting

## Slide 17
Determine resolution for high-res RIXS, #[206273:206277]
Average FWHM = 6.1240375 pxl (from 5 C-tap scans)
Res = 6.1240375 pxl* 0.0037176 eV/pxl = 22.77 meV
Gauss + constant bkg

## Slide 18
Determine resolution for high-res RIXS, #[206273:206277]
Average FWHM_V = 5.80439 pxl (from 5 C-tap scans)
Res = 5.80439 pxl* 0.0037176 eV/pxl = 21.58 meV
Voigt + constant bkg
Average FWHM_V = 5.80439 pxl
Average FWHM_G = 4.34800 pxl
Average FWHM_L = 2.445187 pxl
FWHM_V = 5.80 pxl
Res_V = 21.56 meV

## Slide 19
Determine resolution for high-res RIXS, #[206273:206277]
Combine FWHM = 6.2884684 pxl (from 5 C-tap scans)
Res = 6.2884684 pxl* 0.0037176 eV/pxl = 23.378 meV
Gauss + constant bkg
Combine slightly broadens elastic line?

## Slide 20
Determine resolution for high-res RIXS, #[206273:206277]
Combine FWHM_V = 5.97946 pxl (from 5 C-tap scans)
Res = 5.97946 pxl* 0.0037176 eV/pxl = 22.229 meV
Voigt + constant bkg
FWHM_V = 5.97946 pxl
FWHM_G = 4.53899 pxl
FWHM_L = 2.43405 pxl
Res_V = 22.229 meV
FWHM_G = 16.874 meV
FWHM_L = 9.0488 meV
Combine slightly broadens elastic line?

## Slide 21
Fit all C-tape data for high-res RIXS
Voigt + constant bkg
21K: [206427:2:206451],
63K: [206459:2:206483],
104K: [206490:2:206514,205553,206555],
155K: [206521,206525:2:206551]
Process with Dawn then
“stp1p0_high_res_ctape”
Fit every ctape save result
disp = 0.0037176 eV/pxl

## Slide 22
Fit all C-tape data for ultrahigh-res RIXS
Voigt + constant bkg
22K: [206693:2:206697,206702],
63K: [206704:2:206710],
104K: [206712:2:206718],
155K: [206720:2:206724]
Process with Dawn then
“stp1p1_ultrahigh_res_ctape”
Fit every ctape save result
disp = 0.00236855 eV/pxl

## Slide 25
Grazing-in (norm. to m4c1)
LV (E//ab)
LH (E//c)
px,y
pz
Grazing-in XAS (norm. to m4c1)

## Slide 26
Elastic line fitting of C-tape for all temperatures
High-res
ultrahigh-res

## Slide 27
Elastic intensity from fast Q-scan
fwhm = 0.09456; % estimated from #206366 Qcdw with strong elastic line

## Slide 30
T104, h0.26

## Slide 31
Fit2, Voigt+4Guass (width fixed to res)

## Slide 32
Fit2, Voigt+4Guass (width fixed to res)
Bose factor corrected

## Slide 33
Fit2, Voigt+4Guass (width fixed to res)

## Slide 34
Fit2, Voigt+4Guass (width fixed to res)
Bose factor corrected (use Gauss peak energy)
Should not call y as intensity any more

## Slide 35
Fit3, 5Voigt (width fixed to res)

## Slide 36
Fit3, 5Voigt (width fixed to res)
Bose factor corrected, refit peaks with 4Voigt

## Slide 37
Fit2, 5Voigt (width fixed to res)

## Slide 38
Fit2, 5Voigt (width fixed to res)
Bose factor corrected, refit peaks with 4Voigt

## Slide 39
Fit2, 5Voigt (width fixed to res)

## Slide 40
Fit2, 5Voigt (width fixed to res)
Bose factor corrected, refit peaks with 4Voigt

## Slide 42
Prior RIXS studies of EPC in the 2D cuprates have
focused largely on the Cu L3-edge [30, 35, 37]. How-
ever, it has been established that the bands that cross
the Fermi level in doped cuprates have significant oxy-
gen 2px;y orbital character [38]. Moreover, the phonons
believed to be most relevant to pairing in the cuprates
are the optical oxygen modes [6, 17]. It is, therefore, desirable to also study the EPC at the O K-edge in these
materials.
The RIXS process at this edge involves the
1s-2p transition, so that in the intermediate state the
charge perturbation mostly involves the electron in a 2p
orbital
Why O K-edge has a longer core-hole life time?
Compare to the softening of acoustic mode from IXS measurements?
To the BS mode
To establish that it is not from EPC
And the width is broader then the CDW order
Y. Peng et al., arXiv:2111.05533.

## Slide 45: Experimental probe of EPC
ARPES probes fermionic, the phonon Q-dep is integrated.
NS/IXS relies on lifetime analysis
RIXS as a new route to probe EPC. Phonon inten. EPC and interference with charge
Cu L-edge has been applied widely.
Strong coupling mode: BS, what about lower-energy phonons?
Buckling mode? Bi PNAS paper – Buckling mode interference
What about in stripe ordered compound?

## Slide 48
Coupling of Charge and Lattice Dynamics in Eu-La2-xSrxCuO4, x=1/8
An O K-edge Resonant Inelastic X-ray Scattering (RIXS) Study
Qisi Wang
Johan Chang Group
Group meeting, Jan. 26th, 2022

## Slide 49
Elementary degrees of freedom in quantum materials and their couplings
https://pc.fhi-berlin.mpg.de/docm/research
Neutron scattering
Neutron/x-ray scattering
Resonant x-ray
Scattering / ARPES
Resonant x-ray
Scattering

## Slide 50
Elementary degrees of freedom in quantum materials and their couplings
https://pc.fhi-berlin.mpg.de/docm/research
Neutron scattering
Neutron/x-ray scattering
Resonant x-ray
Scattering / ARPES
Resonant x-ray
Scattering
BCS superconductivity
High-Tc ?
Stripe order ? ...
e-phonon coupling: renormalization of electrons by phonons

## Slide 51
Elementary degrees of freedom in quantum materials and their couplings
https://pc.fhi-berlin.mpg.de/docm/research
Neutron scattering
Neutron/x-ray scattering
Resonant x-ray
Scattering / ARPES
Resonant x-ray
Scattering
M(k,q) depends on fermionic k + bosonic q

## Slide 52
ARPES as a probe of e-ph coupling
Inter-band e-ph
scattering
ARPES kink
EPC constant
Hofmann et al., New J. Phys. 11, 125005 (2009)
Lanzara et al., Nature, 412, 510 (2001)

## Slide 53
ARPES as a probe of e-ph coupling
Inter-band e-ph
scattering
ARPES kink
EPC constant
Hofmann et al., New J. Phys. 11, 125005 (2009)
Lanzara et al., Nature, 412, 510 (2001)
Which bosonic mode? Phonon? Magnon?
q-dependence of M(k,q)?
Which phonon?

## Slide 54
RIXS as a probe of e-ph coupling
2p→3d RIXS process
Braicovich et al., PRR 2, 023231 (2020)
Wang et al., Sci. Adv. 7, eabg7394 (2021)
i) Electron-phonon coupling
ii) Core-hole lifetime
Defining parameters for RIXS phonon intensity
Scattering geometry
RIXS phonon

## Slide 55
L-edge RIXS results on Eu-LSCO: e-ph coupling enhanced in the LTT charge ordered phase
Wang et al., Sci. Adv. 7, eabg7394 (2021)
LTO: low-temperature orthorhombic
LTT: low-temperature tetragonal – ideal structure for stripe order?
Q-dependent e-ph coupling peaks near QCDW
Bond-stretching mode

## Slide 56
Why O-K RIXS for e-ph coupling study
Bands across the Fermi level of doped cuprates have significant O 2px,y character
Pros:
LSCO XAS
Chen PRL 66, 104 (1991)

## Slide 57
Why O-K RIXS for e-ph coupling study
Bands across the Fermi level of doped cuprates have significant O 2px,y character
Low-energy phonons are predicted to strongly coupled to charge order
Pros:
LSCO XAS
Anazai Sci. Rep. (2017)
Chen PRL 66, 104 (1991)
Forgan et al., Nat. Comm. 6, 10064 (2015)

## Slide 58
Why O-K RIXS for e-ph coupling study
Bands across the Fermi level of doped cuprates have significant O 2px,y character
Low-energy phonons are predicted to strongly coupled to charge order
Pros:
LSCO XAS
Low-energy phonons could possibly influence pairing
Anazai Sci. Rep. (2017)
Chen PRL 66, 104 (1991)
Johnston PRB 82, 064513 (2010)
Forgan et al., Nat. Comm. 6, 10064 (2015)

## Slide 59
Why O-K RIXS for e-ph coupling study
Longer core-hole lifetime — larger RIXS phonon cross sections
Bands across the Fermi level of doped cuprates have significant O 2px,y character
Low-energy phonons are predicted to strongly coupled to charge order
Single magnon disallowed — phonons are more isolated
Pros:
LSCO XAS
Low-energy phonons could possibly influence pairing
Anazai Sci. Rep. (2017)
Chen PRL 66, 104 (1991)
Johnston PRB 82, 064513 (2010)
Forgan et al., Nat. Comm. 6, 10064 (2015)

## Slide 60
Why O-K RIXS for e-ph coupling study
Longer core-hole lifetime — larger RIXS phonon cross sections
Bands across the Fermi level of doped cuprates have significant O 2px,y character
Low-energy phonons are predicted to strongly coupled to charge order
Single magnon disallowed — phonons are more isolated
Cons: localized limit of carrier in the intermediate state is not well-satisfied
Pros:
LSCO XAS
Low-energy phonons could possibly influence pairing
Anazai Sci. Rep. (2017)
Chen PRL 66, 104 (1991)
Johnston PRB 82, 064513 (2010)
Forgan et al., Nat. Comm. 6, 10064 (2015)

## Slide 61
Why O-K RIXS for e-ph coupling study
Longer core-hole lifetime — larger RIXS phonon cross sections
Bands across the Fermi level of doped cuprates have significant O 2px,y character
Low-energy phonons are predicted to strongly coupled to charge order
Single magnon disallowed — phonons are more isolated
Cons: localized limit of carrier in the intermediate state is not well-satisfied
Pros:
LSCO XAS
Low-energy phonons could possibly influence pairing
Anazai Sci. Rep. (2017)
Questions: low energy phonon couples to CDW? Any change into the LTT or CDW phase?
Chen PRL 66, 104 (1991)
Forgan et al., Nat. Comm. 6, 10064 (2015)
Johnston PRB 82, 064513 (2010)

## Slide 62
RIXS experiment
DIAMOND light source
I21 RIXS beamline
O K-edge
Energy res. FWHM~ 22 meV

## Slide 63
LV (E//ab)
LH (E//c)
ZRS
UHB
px,y
3d9L->1s3d9
pz
3d9->1s3d10
Grazing-in XAS
XAS: significant O pxy orbital character
Resonance at the Zhang-Rice singlet energy

## Slide 64
Fitting and assignment of RIXS excitations
0
0.5
1
1.5
2
2.5
3
-0.5
Energy loss (eV)
Intensity (a.u.)
dd-excitations
Bi-magnon
Charge order
+ diffuse
phonons

## Slide 65
Fitting and assignment of RIXS excitations
0
0.5
1
1.5
2
2.5
3
-0.5
Energy loss (eV)
Intensity (a.u.)
dd-excitations
Bi-magnon
Charge order
+ diffuse
phonons
h = 0.27
h = 0.18
O K-edge
Cu L-edge

## Slide 66
Fitting and assignment of RIXS excitations
0
0.5
1
1.5
2
2.5
3
-0.5
Energy loss (eV)
Intensity (a.u.)
dd-excitations
Bi-magnon
Charge order
+ diffuse
phonons
h = 0.27
h = 0.18
Excitation energy
Cu L-edge
O K-edge
Bond stretching (half breathing)
DFT
Optical
Chaplot et al., PRB 52, 7230 (1995)
Giustino et al., Nature 452, 975 (2008)

## Slide 67
Fitting and assignment of RIXS excitations
0
0.5
1
1.5
2
2.5
3
-0.5
Energy loss (eV)
Intensity (a.u.)
dd-excitations
Bi-magnon
Charge order
+ diffuse
phonons
h = 0.27
h = 0.18
Buckling A1g
Excitation energy
Cu L-edge
O K-edge
Bond stretching (half breathing)
DFT
Optical
Chaplot et al., PRB 52, 7230 (1995)
Giustino et al., Nature 452, 975 (2008)

## Slide 68
h = 0.27
h = 0.27
h = 0.18
h = 0.18

## Slide 69
Fitting and assignment of RIXS excitations
0
0.5
1
1.5
2
2.5
3
-0.5
Energy loss (eV)
Intensity (a.u.)
dd-excitations
Bi-magnon
Charge order
+ diffuse
phonons
h = 0.27
h = 0.18
Buckling B1g
Buckling A1g
Excitation energy
Cu L-edge
O K-edge
Bond stretching (half breathing)
DFT
Optical
Chaplot et al., PRB 52, 7230 (1995)
Giustino et al., Nature 452, 975 (2008)

## Slide 70
Fitting and assignment of RIXS excitations
0
0.5
1
1.5
2
2.5
3
-0.5
Energy loss (eV)
Intensity (a.u.)
dd-excitations
Bi-magnon
Charge order
+ diffuse
phonons
h = 0.27
h = 0.18
Buckling B1g
Buckling A1g
Excitation energy
Cu L-edge
O K-edge
Bond stretching (half breathing)
Acoustic mode?
DFT
Optical
Chaplot et al., PRB 52, 7230 (1995)
Giustino et al., Nature 452, 975 (2008)

## Slide 71
Elastic scattering: charge ordering
Correlation length comparable to Cu L-edge results
Confirm O states contribute to charge ordering

## Slide 72
E-h dependence of RIXS intensity
Temperature
TLTT = 125 K

## Slide 73
Bose popular factor corrected RIXS intensity
T
TLTT = 125 K
Buckling modes show weak softening and (probably) intensity enhancement near QCDW
T
TLTT = 125 K
Stretching mode
~20 meV mode
Buckling
mode

## Slide 74
Bose popular factor corrected RIXS intensity
T
TLTT = 125 K
~20 meV mode shows a VERY pronounced intensity peak near QCDW
Buckling modes show weak softening and (probably) intensity enhancement near QCDW
T
TLTT = 125 K
Stretching mode
~20 meV mode
Buckling
mode

## Slide 75
Bose popular factor corrected RIXS intensity
T
TLTT = 125 K
~20 meV mode shows a VERY pronounced intensity peak near QCDW
~20 meV mode shows NO obvious softening – e-ph coupling should renormalize the dispersion
Buckling modes show weak softening and (probably) intensity enhancement near QCDW
T
TLTT = 125 K
Stretching mode
~20 meV mode
Buckling
mode

## Slide 76
Bose popular factor corrected RIXS intensity
T
TLTT = 125 K
~20 meV mode shows a VERY pronounced intensity peak near QCDW
~20 meV mode shows NO obvious softening – e-ph coupling should renormalize the dispersion
Buckling modes show weak softening and (probably) intensity enhancement near QCDW
T
TLTT = 125 K
The peak persists beyond the LTT phase – in contrast to the bond-stretching mode
The peak is very sharp in momentum – in contrast to the bond-stretching mode
Bond-stretching
Stretching mode
~20 meV mode
Buckling
mode

## Slide 77
Bose popular factor corrected RIXS intensity
T
TLTT = 125 K
~20 meV mode shows a VERY pronounced intensity peak near QCDW
~20 meV mode shows NO obvious softening – e-ph coupling should renormalize the dispersion
Buckling modes show weak softening and (probably) intensity enhancement near QCDW
T
TLTT = 125 K
Weak coupling expected – spectral weight of the 20 meV mode dominated by heavy elements? Cu, La?
unlikely due to e-ph coupling ...
The peak persists beyond the LTT phase – in contrast to the bond-stretching mode
The peak is very sharp in momentum – in contrast to the bond-stretching mode
Bond-stretching
Stretching mode
~20 meV mode
Buckling
mode

## Slide 78
Mechanisms for RIXS phonon enhancement: coupling to charge excitations
Fano interference with charge continuum?
T
TLTT = 125 K
Stretching mode
~20 meV mode
Lee et al., Nat. Phys. (2020)

## Slide 79
Mechanisms for RIXS phonon enhancement: coupling to charge excitations
Fano interference with charge continuum?
T
TLTT = 125 K
Phonon dispersion is not renormalized
Stretching mode
~20 meV mode
Charge order in Eu-LSCO is more static
Phonon couples to charge goldstone mode?
Why particularly this low-energy mode?
Charge excitations decay quickly into a continuum?
Lee et al., Nat. Phys. (2020)

## Slide 80
This enhanced mode is also seen in LSCO without LTT structure
—charge fluctuations are generic
Mechanisms for RIXS phonon enhancement: coupling to charge excitations
Fano interference with charge continuum?
Lee et al., Nat. Phys. (2020)
T
TLTT = 125 K
Huang et al., PRX 11, 041038 (2021)
Phonon dispersion is not renormalized
Stretching mode
~20 meV mode
Charge order in Eu-LSCO is more static
Phonon couples to charge goldstone mode?
Why particularly this low-energy mode?
Charge excitations decay quickly into a continuum?

## Slide 85
Fit3, 5Voigt (width fixed to res)
Bose factor corrected
Dump this

## Slide 86
Fit2, 5Voigt (width fixed to res)
Bose factor corrected (use Voigt peak energy)
Dump this